Hydrogels Gabriele’s method– Preparation Protocol- Patterns

FV420/128: Preparation of 35mm petri dishes with glass bottom: (do 4-5 at a time)

- N2 gas
- 3-(trimethoxysilyl) propyl acrylate
- 35mm glass bottom petri dishes
- 70% ethanol (wash bottle)
- Deionized water (wast bottle

1. Clean glass bottom with 70% ethanol and dry with N2.
2. Glass bottoms are treated for 1 hour with 3-(trimethoxysilyl) propyl acrylate (10-20µl) to promote strong adhesion between the glass and gels. Spread with pipette tip.
   Put cover on to avoid evaporation. Leave in hood. (Don't let the chemical touch the plastic)
3. After incubation, wash coverslips with 70% ethanol followed immediately with deionized water. Dry the coverslips N2 gas. No stains!
4. Collect liquid waste in waste container and aspirate.

FV420/128 Preparation of 15x15 square coverslip: (do 5-10 at a time)

- 15x15mm square coverslips
- Glass becker
- Glass petri dish
- 70% ethanol
- Sigmacote (new flask and used flask)
- N2 gas
- Sonicator

1. Coverslips in a becker are sonicated 15 min in 70% ethanol, rinsed with 70% ethanol and distilled water, and dried with N2.
2. Place coverslips in the glass petri dish and add Sigmacote to cover the surface.
   The reaction is almost instantaneous. Collect used sigmacote in waste container fill petri dish with sterile type-II water.
3. After incubation, rinse coverslips with 70% ethanol and type-II water to remove HCl byproducts before use. (You may wipe with paper) Dry with N2.

FV431: Preparation of solutions for Hydrogels:
- 2ml Eppendorf
- Pipettes and tips
- FluoSpheres
- 1M HEPES
- Acrylamid
- Bis-acrylamid
- APS
- TEMED

1. Pipette 100 ul FluoSpheres from original bottle into a 2 ml Eppendorf.
2. Dilute original 1M HEPES to 50mM: 250ul of HEPES + 4.75ml PBS in 5ml falcon tube.
3. Pipette 5ml Acrylamid and Bis-acrylamid to 15ml falcon tubes.
4. Mix 10% APS in Eppendorf: 0.2g APS + 2ml sterile type-II water. Store in freezer.
5. Pipette 2ml TEMED to Eppendorf. Store in fridge.

FV431: Preparation of 8kPa Hydrogels: For others see table

- 2 x 2ml Eppendorf
- Cone box + 5-10 Cones
- Pipettes and tips
- 15x15 treated coverslips
- Treated petri dishes
- Large container with distilled water (for 10 dishes)
- Sonicator (FV420)
- FluoSpheres
- HEA
- 50mM HEPES (dilute original 1M in PBS)
- Acrylamid
- Bis-acrylamid
- APS
- TEMED
- PBS
- Parafilm

1. Sonicate Eppendorf with FluoSpheres in 30 min. (Bring to FV420, or move sonicator).
2. Prepare Eppendorf with 1 µL HEA and 1.4 mL and vortex.
3. Follow table for desired rigidity.
4. Mix with vortex before adding APS and TEMED. If you see air bubbles: Go to FV128 and degas solution for 20 min under vacuum.

1. Polymerization starts when APS and TEMED are added.
  1. Claude: Mix slowly with cone (400µL) without inserting bubbles.
  2. Daria: Vortex to mix well
2. Prepare a cone box with a few cones (or use tube rack) and put 15x15 coverslips on top of the cones.
3. Put a 16µL drop (to obtain 70 µm height) of gel solution on the coverslips and bring the Petri dish down slowly to catch the gel solution by capillarity
4. Let the Petri plates float on top of water (to keep humidity) for 20-30 min (until gel polymerizes, check with test solution in Eppendorf).
5. When gel in Eppendorf is gelled, take petri dish from water, turn around and add sterile type-II water for >30 min.
6. Remove the coverslip inside the water on top of the gel carefully with scalpel.
7. Rinse the gel with PBS three times. Leave PBS on gel.
8. Gels can be stored at 4°C for 3 days by sealing Petri plates with parafilm.

FV128: Preparation of Patterns on PDMS:

1. Mix well 9/10 PDMS + 1/10 crosslinker in plastic beaker (%wt 9g/1g on a scale).
2. Degas until bubbles are gone (30 min)
3. Pour the PDMS on the silicon master (height 1mm). Degas again for 30 min. Then cure 2h at 60°C (room 318).
4. Cut the region of interest.
5. PDMS stamps are activated in plasma chamber (Not O2, same protocol as for hydrophilicity).

FV431: Stamping of patterns on gel:
- Fibronectin (Premixed with fluorescent)
- N2 gas
- PDMS stamp
- BSA

1. Put a drop (150-200 µl) of the sterile solution of Fibronectin at 20 µg/mL (laminar hood) 1 hour. (The drop should stay on top of the PDMS square) (mix in fluorescent)
2. Remove the drop with a pipette (or similar)
3. Dry stamps with N2 (not too brutally)
4. Dry gels completely with N2.
5. Press stamps onto the gel for 1 hour at room temperature
6. Remove carefully the PDMS stamp with a tweezer.
7. Other regions are passivated with 1mL BSA (3%= 3g /100 ml in PBS) 1h at room temperature.
8. Wash 3 times with a sterile PBS solution
9. Seed with cells. Cells are added at high concentration for 30 min, before 3 mL of medium is added.